More set 1 problems

- One of the images below shows a predominantly transgranular fracture and the other a predominantly intergranular fracture in a 7050 alloy.  Which is which?  Explain.

10.  Find the crack origin in the image below.

11.  How did this Q + T 9310 pin fail?  How was it loaded?  Explain.

12.  Ductile or brittle fracture?  Why?

- Characterize Al alloys in general by listing their strengths and weaknesses.

- What is the composition of 7075?

- Which 5457 alloy has been most heavily cold-worked?

16.  Ageing, solution treat, and quench are the three steps in precipitation or age hardening of alloys.  Put the three steps in the correct order and describe what happens inside the material during each step.