MatSE 259 - Third exam Fall 2005

Put student number on answer sheet

Only one correct answer for each question

Turn in test questions paper with answer sheets

For problems 1-4, match with a-e below

a.

b.

c.

d.

e.

1.  Polyester

2.  Polyethylene

3.  Nylon

4.  Bakelite

5.  Which polymer in a-e above is branched?

6.  Which polymer in a-e above polymerizes by addition?

7.  Which polymer in a-e above has an ester group?

8.  Which polymer in a-e above is not thermoplastic?

- Below is shown one of the welded joints in a 6061-T6 (Al w/ Mg & Si) bicycle frame.  Diamond pyramid hardness values, determined after the welding, at various points near the weldment (region C) are given.  Which region is overaged?  The diagram on the next page should help jog your memory on age hardening.

10.  Which shows the microstructure of a ductile cast iron?

a.

b.

c.

11. What purpose does chromium serve in chromium plating?

a. to smooth the metal surface

b. to make the metal surface look good (correct)

c. to protect the metal underneath

d. to prevent crevice formation

12. Determine the best quenching medium to obtain a hardness of RC37 at a depth of 0.2 from the surface in a 2” diam. 4640 bar.  The 4640 Jominy curve I given below.

a. water

b. oil

c. air

d. brine

13. Reason for use of a ceramic cutting tool

a. can’t afford the more expensive types of tools

b. the work material is very soft

c. the work material is very hard

d. need a tool that doesn’t fracture easily

14.  For the corrosion example shown below, what type of cell is probably NOT responsible for the corrosion?

a. concentration

b. dissimilar metals

c. non-homogeneous residual stress

d. none of the above

15.  Best method for suppressing corrosion in an underground carbon steel water line

a. cathodic protection

b. sacrificial anode

c. Cr plating

d. sensitization

e. passivation

16.  Candidate material for induction hardening

a. 1020

b. 6061-T6

c. 1008

d. 4340

17. Quench and temper not required

a. pack carburizing

b. gas carurizing

c. nitriding

d. carbonitriding

18.  Corrosion “microcell”

a. deep scratch in galvanized coating

b. deep scratch in noble metal coating

c. 6061-T6

d. bent nail

e. deep scratch in painted steel surface

19.  Below are side and end views of a portion of a polyvinyl chloride (PVC) molecule.  The large spheres represent the chlorine atoms.  The molecule is

a. attacktic

b. atactic

c. syndiotactic

d. isotactic

e. monotactic

20. Which is correct?

a. when scratched, noble metal coatings corrode

b. when scratched, the metal underneath a noble metal coating corrodes

c. when scratched, sacrificial metal coatings corrode

d. when scratched, the metal underneath a sacrificial metal coating corrodes

e. no corrosion occurs when coating scratched

21.  What is the polymer molecule shown below

a. a polyester

b. polypropylene

c. nylon

d. polyethylene

e. branched polyethylene

22.  Which stainless steel can be sensitized?

a. 321

b. 347

c. 304L

d. 304

e. all of the above

23.  Molecular weight of a polyethylene chain containing 8000 ethylene units (C -12, H – 1)

a. 8000

b. 1012

c. 28

d. 112,000

e. 224,000

24. Which is correct

a. the yield strength for all types of materials is determined from the

stress-strain curve in the same manner

b. the yield strength for a number of steels is not determined by the

0.2% offset method

c. the yield strengths for ceramic materials are known

d. the impact energy for most steels is less than that for ceramic

materials

25.  Best definition for “heat treatment”

a. a process in which a material is softened

b. a process in which a material is strengthened

c. a process in which a material is quenched from a high temperature

d. a process in which the structure of a material is changed by subjecting

it to a series of temperature changes

e. a process designed to change the elemental composition of a material

# Text boxes

C

B

A