MatSE 471

## Laboratories 7-8

# Tempering of Lath Martensite

1. Objective

The objective of this laboratory is to monitor the changes that occur during the tempering of a steel using Rockwell hardness testing, microhardness and metallography.

2. Background

When a low to medium carbon steel is quenched sufficiently rapidly, it transforms by shear to lath martensite (a slightly distorted A2 structure (ex: -Fe) phase). Martensite is very hard and extremely brittle. Because of this brittleness, it is normally tempered prior to use to imbue the material with toughness, while maintaining the hardness, usually, at a variety of high levels. The various changes that occur during the tempering of ferrous martensites are summarized in Table 1. The temperature intervals are very approximate and considerable overlap occurs between each range. Similar information is also presented in Figure 1, which plots hardness as a function of tempering temperature, and also outlines the temperature regions within which each reaction occurs.

Table 1

Transformations Occurring During Tempering of Ferrous Martensites

(After G.R. Speich in Metals. Handbook. 8th edn.. vol. 8. American Society for Metals, Metals Park. Ohio, 1973

| Temperature(C | Transformation | Remarks |
| --- | --- | --- |
| 25-100 | Carbon segregation to dislocations; pre-precipitation clustering | Clustering predominant in high-carbon steels |
| 100-250 | Epsilon-carbide precipitation (first stage of tempering) | May be absent in low-carbon, low-alloy steels |
| 200-300 | Retained austenite transforms to bainite (second stage) | Occurs only in medium-carbon and high-carbon steels |
| 250-350 | Lath-like Fe3C precipitation (third stage) |  |
| 400-600 | Recovery of dislocation substructure. Lath-like Fe3C agglomerates to form spheroidal Fe3C | Lath structure maintained |
| 500-600 | Formation of alloy carbides. (secondary hardening or fourth stage) | Occurs only in steels containing Ti, Cr, Mo, V, Nb, or W; Fe3C may dissolve |
| 600-700 | Recrystallization and grain growth; coarsening of spheroidal Fe3C | Recrystallization inhibited in medium-carbon and high—carbon steels; equiaxed ferrite formed |

Now, time and temperature have related effects on tempering.  This is shown in figure 2.  From figure 2, it can be seen that the data can be related by a simple rate equation:

1/t = A exp (-Q/RT)

where t is the time to attain a given hardness, A is a constant, Q is an empirical activation energy, and R and T have their usual meanings.

Figure 1.  The hardness of low and medium iron-carbon martensites tempered for 1 hour between 100°C and 700°C.

Figure 2.  The effect of time and temperature on the hardness of a tempered 0.82C-0.75Mn steel.

- Procedure

This is a two-week laboratory and the following tasks will be performed in weeks 1 and 2.

  - Week 1

You will be provided with two steel samples.

Austenitize them at 1000°C for 10 minutes and quench into ice brine.  Measure the hardness of the samples.  Temper the samples for one hour at 650°C* and again ice-brine quench.  Measure the hardness of the quenched and tempered specimens.

In addition to the above, you will be provided with a series of samples which have already been heat treated.  The heat treatment schedule is provided in Table 2.  Measure the hardness of all the samples to produce a plot of hardness versus tempering time.

Table 2.  Quenched and Tempered Samples

| 1035 | 1000°C | 45 min | water quench |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| 1035 | 1000°C | 45 min | water quench | 650°C | 1 hr | Air Cool |
| 1035 | 1000°C | 45 min | water quench | 650°C | 2 hr | Air Cool |
| 1035 | 1000°C | 45 min | water quench | 650°C | 5 hr | Air Cool |
| 1035 | 1000°C | 45 min | water quench | 650°C | 10 hr | Air Cool |
| 1035 | 1000°C | 45 min | water quench | 650°C | 20 hr | Air Cool |
| 1035 | 1000°C | 45 min | water quench | 650°C | 40 hr | Air Cool |
| 1035 | 1000°C | 45 min | water quench | 650°C | 100 hr | Air Cool |
| 1035 | 960°C | 30 min | water quench |  |  |  |

Additionally:

- Compare the hardness results of your quenched and quenched and tempered samples with those that are provided for you. Discuss the reasons for the differences.

- For one particular sample, produce a sufficient number of indents so that the errors in the hardness numbers can be evaluated.

3.2  Week 2  (Lab 8)

You will be provided with a quenched and tempered specimen.  Polish, etch, and obtain an image of the microstructure.  Obtain microstructure images for all the samples listed in Table 2.  Do microhardness testing on the 100 hr specimen to determine whether or not there are significant variations in hardness from one region to another.  Interpret your results in your report.

*For both austenitizing and tempering, monitor the temperature using a thermocouple.