Name________________________________

Grade____________________/10

MAT SC 530

HOMEWORK # 5

1.	Consider iron flakes that are extended along the (200) plane and thin in the [001] direction.  Iron has an easy axis in the [100] direction.  If the flakes are dropped onto the flat surface of a specimen holder,

a)	Draw the -2 x-ray diffraction pattern expected.

b)	Draw the -scan of the (110) x-ray diffraction peak expected.

If a magnetic field is now applied in the plane of the deposit,

c)	Draw the -2 x-ray diffraction pattern expected.

d)	Draw the -scan of the (110) x-ray diffraction peak expected.

2.	The measured -2 and -scans for two platinum (F cubic) thin films are shown below.  The first set of plots is for a platinum film grown on a silicon single crystal and the second set is for a platinum film grown on a SrTiO3 single crystal.

a)	Which film(s) is(are) epitaxial?  Why?

b)	For the epitaxial film(s) specify the orientation relationship.  Show how you arrived at 			your answer.