- Construct, to scale, the l = 0, 1, 2 layers of the reciprocal lattice for an orthorhombic crystal for which a = 5, b = 7 Å.  Let h, k run over the range  2.  Index each point.  Show the unit cell in each layer and mark the unit cell axes.

2.  An almost infinite number of tiny, perfectly cube-shaped grains of salt, about 1 micron in size, are dropped onto a flat glass plate so that they are extremely densely packed. For NaCl, a = 5.64 Å.

Construct, to scale, a drawing of the representation of the reciprocal lattice for this specimen, index, and explain.

When cubes fall onto plate, they will all lie on a cube face.  This means that they will have a “preferred orientation”, like this:

Note that all cubes have one crystal direction in common, perpendicular to the plate (we might even think of this as a zone).

The reciprocal lattice for one crystal is (NaCl is F cubic, and certain crystal planes for F don’t exist):

The representation of the reciprocal lattice for the many crystals is then obtained by rotating the above lattice about [001]:

- Calculate the critical voltage necessary to produce characteristic FeK radiation in a conventional laboratory x-ray tube.

voltage (kV) = 12.4/lKedge (Å) = 12.4/1.74334 = 7.11 kV

- Calculate the energy for CrKa and CuKa X-radiation.  What elements should be used as b-filters for Cr and Cu X-ray tubes?

Cr:  energy (keV) = 12.4//l (Å) = 12.4/2.29092 = 5.41 keV

Cu:  energy (keV) = 12.4//l (Å) = 12.4/1.541838 = 8.04 keV

- Calculate the mass attenuation coefficient for the compound SiO2 for CuKa radiation.

(wt. fraction)Si = 28/60 = 0.467, (wt. fraction)O = 0.523

µSi = 60.6       µO = 11.5

µSiO2 = (wt. fraction)Si x µSi + (wt. fraction)O x µO

µ SiO2 = 0.467 x 60.6 + 11.5 x 0.523 = 34.3 cm2/gm

- Calculate   (= = mass attenuation coefficient;  * = linear attenuation coefficient) for air for CrK radiation.  Plot the transmission factor = e-x for path lengths of 0-20 cm.  Assume that air is 80 % nitrogen and 20 % oxygen by weight, with a density of 1.29 × 10-3 .

# Text boxes

l = 0

000

100

200

100

200

210

220

110

210

210

220

110

210

210

120

220

220

110

110

120

120

010

010

020

020

021

021

011

011

121

121

111

111

121

221

221

111

211

211

211

221

221

111

211

211

101

201

101

001

l = 1

201

022

022

012

012

122

122

112

112

122

222

222

112

212

212

212

222

222

112

212

212

102

202

102

002

l = 2

202

220

020

200

111

[001]

[001]

111

200

020

220

220

200

202

222

111

Answer;

(rings repeat along [001]