1.  An almost infinite number of tiny, perfectly cube-shaped grains of salt, about 1 micron in size, are dropped onto a flat glass plate so that they are extremely densely packed. For NaCl, a = 5.64 Å.

Construct, to scale, a drawing of the representation of the reciprocal lattice for this specimen, index, and explain.

(You did this before.)

Now make the glass plate + NaCl crystals the specimen in a powder diffractometer.  Do the Ewald construction (CuKa radiation) for such a specimen to see what the powder pattern would look like.  Draw and describe the pattern.

From the last problem set:

Now, the Ewald construction is:

Since powder diffractometer is

a 2-D instrument, can just use a

circle for Ewald construction.

As diffractometer rotates,

many of the points will come to lie

on Ewald circle, but counter will

only be in right place to detect

(00l) reflections (with l = odd extinct)

- Determine the angle settings (crystal angle and counter angle) for a graphite monochromator for FeKa radiation.

c = 2d002 = 6.708 Å      l/2d002 = sin q002

- 1.937355/6.708 = 0.2888 = sin q002; q = 16.78°, 2q= 

- Index these patterns and calculate approximate lattice parameters for each material. (CuKa radiation)

- Derive the extinction rule for C-centering by calculating which (hkl)s systematically have F = 0.  Follow the procedure discussed for I-centering in class.  State the rule in the same form as that given in class.

For every atom at (x,y,z)  there must be one at (x + ½,y + ½,z)

Then:

N/2

F = ( f (exp(2πi (hxj +kyj+lzj)) + exp(2πi (h(xj+1/2) + k(yj+1/2) + lzj)))

j=1

Breaking exponents apart, and reassembling:

N/2

F = ( f (exp(2πi (hxj +kyj+lzj)) (1 + exp(πi (h +k)))

j=1

rule: (hkl), h + k = 2n (even)

- Derive the extinction rule for a 21 screw axis in monoclinic by calculating which (hkl)s systematically have F = 0.  For this screw axis, for every atom at (xj,yj,zj), there must be a symmetry-equivalent atom at (-xj,yj + 1/2,-zj).  State the rule in the same form as that given in class.

For every atom at (x,y,z)  there must be one at (-x,y + ½,-z)

Then:

N/2

F = ( f (exp(2πi (hxj +kyj+lzj)) + exp(2πi (-hxj + k(yj+1/2) - lzj)))

j=1

Can’t do anything to reduce this unless h,l = 0.  Then:

N/2

F = ( f (exp(2πi (hxj +kyj+lzj))(1 + exp(πi k))

j=1

rule:  (0k0), k = 2n

# Text boxes

111

200

210

211

220

221

311

222

111

200

210

211

a=7.84Å

a=5.77Å

220

221

311

222

321

400

410

111

200

220

311

222

400

331

420

a=7.27Å

not cubic

111

200

220

222

400

a=8.93Å

331

422

002

001

004 – 66.29°

002

002 – 31.73°

006 – 110.29°

200

220

111

311

202

222