1.   How does Fhkl change for centrosymmetric structures?  Show your derivation step by step.  Can the x-ray reflection intensities for centrosymmetric structures be used to directly calculate the electron density distribution?

2.	   The diffraction pattern below was obtained from a common cubic material using CuKa radiation.  Determine the Miller indices for each reflection ("index the pattern"), and thereby determine the centering type for the lattice from an inspection of the systematic absences.  Calculate the lattice parameter, a.

To index the pattern, guess the (hkl)'s for the first two or three reflections for P, I, and F cubic, and calculate the corresponding a values for these reflections.  Since this cubic material has a single lattice parameter, the assignment of indices which gives a values which are very close to each other is the correct one.  You will run into an additional problem here; in attempting to solve the problem, do not use h,k,l values higher than 5.  In indexing the pattern, remember that the objective is to find some set of indices (hkl) that gives essentially the same lattice parameter for all reflections.

d(Å)	(hkl) for P	(hkl) for I	(hkl) for F

3.157

1.931

1.647

1.366

1.253

1.1150

1.0512

0.9657

0.9233

0.9105

0.8637

0.8330

- The most precise values of lattice parameters are those obtained for reflections which occur at high angles.  In fact, all errors can be eliminated at  = 90°, and lattice parameter values generally reported are those obtained from an extrapolation of the data to  = 90° against some function intended to make the lattice parameter variation linear.  Two such functions, obtained through an extensive evaluation of systematic experimental errors, are the Bradley and Jay function, cos2 (frequently used for diffractometer data, and truly linear only over the range  = 60-90°) and the Nelson-Riley function (cos2/sinq + cos2/, linear over the range 30-90°, and used for other instrument geometries).

Here are some observed data for a-iron.  Determine the best lattice parameter to 5 decimal places by extrapolating the a values versus cos2qin a graph.  lCuKa1 = 1.5405981 Å.  To index the pattern, remember that a-iron is I cubic.

q	d	(hkl)	a	cos2q

22.3360

32.5114

41.1675

49.4742

58.1948

68.5881

4.  For the data below, determine the weight fractions of rutile and anatase present in a mixture.

Pure rutile:

Reflection	Intensity	Background

1	102309	1508

2	47564	1453

Rutile in the mixture:

Reflection	Intensity	Background

1	36987	1486

2	17408	1439

5.  A rock specimen was analyzed for -quartz.  To correct for the unknown absorption of the specimen, an internal standard was used.  The internal standard was chosen as KCl because of its excellent crystallinity, relatively simple diffraction pattern, and a strong reflection which is relatively close to the strong -quartz reflection.

Three samples were measured:  pure KCl, pure quartz and a mixture of the rock specimen with KCl.  The mixture was prepared by intimately mixing 200 mg of finely ground KCl with 1000 mg of the rock, also finely ground.

The intensities of the 3.15 Å KCl reflection and the 3.34 Å quartz reflection were measured using CuK radiation.  The data are given below.

Phase	d (Å)	o	Pure compound	Mixture

quartz	3.34	35.0	48360 cps	2648 cps

KCl		3.15	124.0	19072	6160

For all intensities, the background was 240 cps.  The dead time for the counting system was 1.0 sec.

The correction for the dead time, , makes use of the following equation:

true counts/sec =

Calculate the concentration of quartz in the rock specimen.

Note that:

where:

I  and Ia are the intensities for the pure compound and the mixture for phase a, respectively.

and  are the mass attenuation coefficients for the pure compound and the mixture, respectively.

X is the weight fraction of phase  in the mixture.

An equation of this type can be written for both quartz and KCl.  Combining these two equations to eliminate , the unknown mass attenuation coefficient for the mixture:

Xq = XKCl

First calculate the weight fraction Xq of quartz in the diluted specimen.  Then, from the value of Xq and the dilution factor, calculate the weight fraction of quartz in the original mixture.

6.  MoB is I41/amd with a = 3.110, c = 16.95 Å, and Mo and B atoms in 8e, z = 0.196 and 0.352, respectively.

Calculate F001 and F004.

F001 = ______

Fhkl = fj exp(2πi(hxj + kyj + lzj)).

F004 = ?

What must be calculated?

d004 = _______

(sin )/ = ________

0.0	0.1

Mo	38.2	32.6

3.5	  2.4

ƒMo = _______

ƒB = _______

8e:  (00z)  (0,,+z)  (,0,-z)  (,,-z)

F004 = _______

7.   -Np is P4212 with a = 4.897, c = 3.388 Å, and Np in 2a ((000) and (0)) and 2c ((0z) and (0)), z = 0.375.  Find I101 for CuK radiation.  Ignore absorption and temperature factor.

ƒ calculation:

(sin )/	0.0	0.1	0.2	0.3	0.4	0.5	0.6	0.7

ƒ			93	87	78	69	60	53	48	44

F calculation:

What is p?

LP calculation:

I calculation: